## Slide 1: INNOVEEA
Activities at HZB
Annual INNOVEEA meeting 10th Nov 2021
O. Kugeler, HZB
WP2
SRF technology

## Slide 2: Sustainability goal: Efficient SRF operation in cw mode
Improve sustainability of niobium cavities for 2-K operation
Eliminate / reduce hazardous HF treatment
Reducing the RF surface resistance: e.g. nitrogen infusion
Develop systems for 4-K+ operation
conduction cooling of SRF cavities rather than LHe
proof-of-principle experiments, on samples
proof-of-principle experiments with simple cavity and some RF
use of new superconductors … development as part of collaborations, i.e. EU-ARIES, BMBF-SMART, EU-IFAST, BMBF-NOVALIS (proposed)
complimentary to in-house research (QPR)
INNOVEEA

## Slide 3: Tasks
Electrodeposition of copper onto Nb (talk Alena Prudnikava)
HF free etching of Nb
Conductive cooling with Cu plated Nb (joint effort with KIT)

## Slide 4: Task 2: Quadrupole Resonator (QPR)
Tool at HZB to characterise RF performance of flat samples (415, 845, 1285 MHz)
Operated in vertical cryostat
  LHe bath at 1.8 K
Coaxial structure
  thermal decoupling
  calorimetric measurement of surface resistance
TSample = 1.8 K … > 20 K
BSample, max (415 MHz) ~ (TESLA)
INNOVEEA
Pumping port
Coupler ports
Calorimetry chamber
4 hollow
rods (Nb)
LHe
Cavity (Nb)
Frame
(SS, Ti)
Coaxial gap
Sample
Pole shoes

## Slide 5: WP2: HF free etching of Nb
Investigating metallographic polishing in collaboration with CEA to evaluate possibility of omitting electrochemistry step in the cavity surface preparation recipe.
INNOVEEA
Pictures courtesy Oleksandr Hryhorenko
QPR sample milled from ASTM0 large grain material
Sa = 7 µm
Poor RF performance
Mirror polishing at IJCLab
Sa = 0.5 µm
Great RF performance of baseline sample
(9 Ohm residual resistance at 416 MHz)
After EP 150 µm + annealed at 900°C under vacuum + EP 20 µm at CEA
Sa = 1 µm
Omit this step and re-evaluate performance

## Slide 6: Task 3: Beyond the limits of niobium
 |  |  |  |  | RBCS @ 1.8 K | RBCS @ 4.2 K
Nb | 9.25 K | 1.5 meV | 39 nm | 32 nm | 3 nΩ | 763 nΩ
Nb3Sn | 18 K | 3.4 meV | 90 nm | 7 nm | << 1 nΩ | ≤ 12 nΩ
NbTiN | 17.3 K | 2.8 meV | 150 -200 nm | 5 nm | << 1 nΩ | ≤ 60 nΩ
 |  |  |  |  | RBCS @ 1.8 K | RBCS @ 4.2 K
Nb | 9.25 K | 1.5 meV | 39 nm | 32 nm | 3 nΩ | 763 nΩ
Nb3Sn | 18 K | 3.4 meV | 90 nm | 7 nm | << 1 nΩ | ≤ 12 nΩ
NbTiN | 17.3 K | 2.8 meV | 150 -200 nm | 5 nm | << 1 nΩ | ≤ 60 nΩ
New materials: Large sc energy gap , large
Control residual resistance
  Intrinsic contribution?
  Cooling conditions, trapped flux
Prevent early vortex penetration
  Multilayer structures
Reducing the RF surface resistance

## Slide 7: Task 3: Conduction cooling of SRF cavities
InnoveEa
Vacuum (Beam) +RF eigenmode
Nb3Sn or other SRF material layer
Nb host cavity (should be avoided if possible)
Cu coating for heat transport
2x thermal
contacts
Transition to cooling media:
Braze or weld connection
Transition/contact between cooling media and e.g. pipe/surface
2x thermal
contacts
In worst case 4 thermal contacts/transitions, which might hinder the heat transport before reaching steady state

## Slide 8: Surface RF losses in SRF Cavities
InnovEea
µW/cm²
Parameter: Maximum field on beam axes 28 MV/m, peak surface magnetic field 60 mT Superconducting surface resistance 12.3 nW at 1.8 K, total dissipated power 1.1 W  Q0=2.2e10 Stored energy in mode 3.05 Joule, but there is more about it…..
TM010 type of RF
Eigenmode with axial symmetry in
azimuthal direction: Main mode applied in particle accelerators
TM010 E-field
TM110 E-field
Power density [µW/cm2]

## Slide 9: How to cool? Some ideas and basic studies
InnoveEa
1st case: Only 0.75 mm Cu thick (!) coating and beam tube end flange cooling to 4.2 K
 Losses increase by factor of 3
 Thermal runaway?
2nd case: “End-cooling” and additional
Cooling at stiffening ring position, Cu coating (0.75mm) only between
Cooling rings
Tmax ~ 4.3 K
Dissipated average power total surface 4.3 W in all cases
3rd case: “End-cooling” plus some 2 mm diameter Cu connectors
to 4.3 K ring every 45 degree
Tmax~4.5 K
Note: All simulations static, cooling boundaries fixed to 4 K, adiabatic boundaries to all directions, no thermal feedback
of dissipated power vs. surface resistance as a function of temperature, no assumption of thermal contact properties
Equator cooling connectors might be flexible braids later
Cu coating (0.75 mm)
 Good enough for dynamic response?
Tmax~5.6 K

## Slide 10: Thank you.
Acknowledgement
Contributions from:
Oleksandr Hryhorenko, Dmitry Tikhonov, Axel Neumann, Sebastian Keckert
INNOVEEA