## Slide 1: Substrate Influence on the Fano coupling of bright-dark modes in THz plasmonic n-doped Ge antennas
Institute of Leibniz Association
Elena Hardt, Carlos Alvarado Chavarin, Soenke Gruessing, Oliver Skibitzki, Thomas Voß, Davide Spirito, Bernd Witzigmann, and Giovanni Capellini
25.11.2022

## Slide 2: Agenda
1
2
3
4
5
6
Motivation/Introduction
Materials
Wavelength: THz Gap
THz-TDS measurement setup
Substrate influence
Coupling Bright-Dark mode: Fano resonance
7
Conclusion

## Slide 3: 1.Motivation/Introduction
THz biosensing
microfluidic integration
lab-on-a-chip
CMOS compatible materials
biosensing platform development
E. Hardt et.al., Opt.Exp.2022, https://doi.org/10.1364/OE.469496
C. A. Chavarin et.al., Opt.Exp.2021, https://doi.org/10.1364/OE.418382
C. A. Chavarin et.al., Freq.2022, https://doi.org/10.1515/freq-2022-0078
blood,
plasma,
serum, etc.

## Slide 4: 1.Motivation/Introduction
Protein
Data analysis
TERASMART tool
THz-TDS
Transducer
Materials
THz
Results
Wavelength
Optic sensor
THz spectroscopy
Label-free THz detection of biomoleculs (proteins)
Technique

## Slide 5: 2.Materials
Si, Ge, SiO2, Si3N4
using CMOS processes in an industry-standard Si foundry pilot line
=> compact, low-cost sensor system
=>mass production
6mm
Si
Si3N4
30-60 nm
Si substrate
SiO2
2000 nm
220 nm
Si
SOI substrate
Ge
1.5 µm
~730 µm
Materials
bow-tie antennas

## Slide 6
THz GAP
100MHz
1GHz
10GHz
100GHz
100THz
1000THz
freq
radio waves
micro waves
Far IR
near IR
visible
1THz~1ps~300µm~33cm-1~4.1meV~47.6°K
doi.org/10.1002/advs.202105932
Membranes and Membrane proteins
DNA and RNA
Enzymes and enzymes catalysis
Cell and tissue imaging
Protein structure and dynamics
10THz
THz range
DOI 10.1007/s10762-009-9561-z
3.Wavelength: THz Gap
Photonics
Electronics
Wavelength
doi:10.4329/wjr.v3.i3.55
very low photon energy=> insufficient to cause chemical damage to molecules
very sensitive to polar substances
intermolecular vibrations such as hydrogen bonds exhibit different spectral characteristics

## Slide 7: 3.Wavelength: THz Gap
THz range 0.1-2.5 THz
(Optical Wavelength ~120-3000µm)
LSPR (Localized surface plasmon resonance) for enhancement of electrical feld
  =>plasmons are collective oscillators of the free
  =>biomoleculs sensing at very low concentrations
THz plasmonic resonators
Biomoleculs (~nm)
HIV-1 Virus ~120nm
Protein ~5nm
DNA ~2nm
Elena Hardt et.al., Opt.Exp.2022, https://doi.org/10.1364/OE.469496

## Slide 8: 4.THz-TDS measurement setup
fs-laser
Sample
Bias
PC
A/D
Amplifier
Emitter
Detector
Transmission mode
Linearly polarized light
x
y
Technique

## Slide 9: 5.Substrate influence: Material
Si
Ge
n-doped (1019 cm-3 )
air
Si3N4
Si
air
Si3N4
SiO2
Si
~d=730 µm
Fabry- Perot
air
Si
incident
reflected
transmitted
Si3N4
phase change of
/2
SiO2
Si3N4
air
Ge
Si
Si
amplitude of incident
>
reflected
>
transmitted
Si3N4
air
Ge
n-doped (1019 cm-3 )
Si
y
x

## Slide 10: 5.Substrate influence: Material
Si3N4
air
Ge
n-doped (1019 cm-3 )
Si
SiO2
Si3N4
air
Ge
Si
Si
Plasmonic resonance
Bright mode

## Slide 11: 5.Substrate influence: Thickness
Oscillations
Not clear from which thickness we have Fano resonance
Si
729 µm
533 µm
331 µm

## Slide 12: 5.Substrate influence: Thickness
Fano resonance?
Si
729 µm
533 µm
331 µm
Si
194 µm
150.6 µm
112.3 µm

## Slide 13: 6.Coupling Bright-Dark mode: Fano resonance
Si
729 µm
533 µm
331 µm
54.6 µm
Very clear Fano resonace
Quality (Q)-Factor
Si
194 µm
150.6 µm
112.3 µm

## Slide 14: 6.Coupling Bright-Dark mode: Fano resonance
Fanocoupling
54.6 µm
Fanoresonace
Fanocoupling effect
1. Bright mode: Plasmonic resonance in Ge antennas
2. Dark mode: Substrate resonance only possible due interaction with the bright mode
Mikhail F. Limonov, Advances in Optics and Photonics, https://doi.org/10.1364/AOP.420731
Substrate resonance
Plasmonic resonance
Fano resonance
Si
729 µm
43.3,
55.3,
65.4 µm

## Slide 15: 7.Conclusions
high n-doped Ge antennas=> Plasmonic resonance in THz light
decrease of substrate=> Fano coupling effect
Fanoresonance=> an improvement of the antenna quality factor (Q-factor) by Fano coupling of bright and dark modes

## Slide 16
Elena, Hardt
249
hardt@ihp-microelectronics.com
681

## Slide 17: BSA detection c = 10mg/mL
Si substrate
SOI substrate
air
air
BSA
BSA
+BSA
Substrate thickness ~730 µm
Substrate thickness ~75 µm
The absorption coefficient(α):

## Slide 18: Sample fabrication
Si substrate
Ge
1.5 µm
* Photoresist
Si3N4
30 nm
Cleaning
Epitaxy Layer
high doped Ge
CVD
Si3N4
30 nm
SiO2
210 nm
* Maske
PE CVD
Exposure
PE CVD
Dry etching, removal of mask,
photoresist and silicon dioxide