## Slide 1
solvent vapor density
ϕS,surf = 0.04
ϕS,surf = 0.12
ϕS,surf = 0.22
ϕS,surf = 0.30
evaporation rate
χSGN0 = 0
χSGN0 = 20
χSGN0 = 35
χSGN0 = 40
Homogeneous Electric Field
Developed as new feature in SOMA
Effectively shifts order-order transition (OOT)
During EISA simulations
  Alignment
  Cylinder growth
Effective Gas Affinity
Solvent selective for majority block
Evaporation: Selective solvent „vapor“ at surface, ϕS,surf
Oliver Dreyer, Dr. Maryam Radjabian, Institute of Membrane Research – Self-Assembly and Functional Nanostructures (PMB), Prof. Dr. Volker Abetz, Institute of Membrane Research – Head of Institute (PM)
Simulating Evaporation-Induced Self-Assembly of Diblock Copolymer Solutions: Identifying Key Parameters
Helmholtz-Zentrum Hereon • Max-Planck-Straße 1 • 21502 Geesthacht I Germany • T +49 4152 87-0 • contact@hereon.de • www.hereon.de
Contact: Oliver Dreyer, Dr. Maryam Radjabian • T +49 4152 87-2212 / 2802 • oliver.dreyer@hereon.de, maryam.radjabian@hereon.de
Introduction
Simulation box and typical polymer architecture
„DIGIZWIMEM“ (I²B) & „MExMeMo“ (BMBF)
Motivation: Understand the interplay of parameters and processes during diblock copolymer membrane formation  digital twin
Current goal: Identify which parameters influence the resulting morphology during evaporation-induced self-assembly (EISA)
Open source simulation tool: SOMA – „Soft Coarse-Grained Monte-Carlo Acceleration“[1] (particle-based)
Aligning the cylindrical morphology[2,3]
Evaporation Rate
Adjusted by repulsiveness between solvent and gas, χSGN0
High evaporation rates favor perpendicular alignment
[1] Schneider, Müller, Comput. Phys. Commun., 2019, 235, 463-476.
Proposed Structure Formation Mechanisms
Concentration gradient forms during evaporation
  Governs polymer morphology
  Determination of spherical and cylindrical layers
Emergence and growth rate of spherical and cylindrical layer govern final morphology
Dependent on concentration gradient
Directly linked to experimentally accessible parameters
1D density profiles of evaporation simulations at early (7 τR) and later stage (55 τR).
Simulation Setup
Chemical species: Polymer A-B, Solvent S, Gas G
Conversion scheme (SG) mimics solvent evaporation
Time evolution of an evaporation simulation
Proposed mechanisms (LEM) for stacked layers of spheres (Scheme A), perpendicular cylinders (Scheme B) and parallel cylinders (Scheme C)
electric field strength
Alignment
  EF aligns permittivity interface along its direction
Cylinder growth
  Captured by LEM
  OOT shift increases cylindrical layer
  Increased growth rate during structure formation
Layer Evolution Model (LEM)[2]
[2] Dreyer, Ibbeken, Schneider, Blagojevic, Radjabian, Abetz, Müller, Macromolecules., 2022, 55, 7564.
[3] Dreyer, Schneider, Radjabian, Abetz, Müller, Macromolecules., 2023, 56, 6880.
without electric field
with electric field