## Slide 1
Thin septum
Thick septum
Beam dump
Storage ring
Transfer line
Permanent and pulsed septa for SLS 2.0
M. Paraliev
Swiss Light Source (SLS) part of
Paul Scherrer Institute,
Switzerland
Injection straight

## Slide 2
Motivation
Injection in small dynamic aperture
Due to the new SLS 2.0 low emittance lattice the beam acceptance of the machine is reduced. A thin septum should make the conventional 4-kicker bump injection possible [1].
Top-up injection transparency
Advanced injection modes like fast injection and on-axis injection will improve further top-up injection transparency [2].
Beam dump
Due to the much smaller dispersion in the arcs (compared to SLS 1) an RF phase inversion-based beam dump might not be acceptable, causing beam loss and irradiation of sensitive devices like superconducting superbends and in-vacuum undulators. To avoid deterioration or damage, a dedicated beam dump magnet should deflect the beam towards well shielded beam dump.
Improved septa
Fast injection elements
Dedicated beam dump

## Slide 3
SLS 2.0 Advanced Injection Schemes
Septum
“Fast” injection scheme, aperture sharing
Simplified illustration of “Fast” injection scheme with aperture sharing (off-axis injection)
Stored beam on-axis
Injected bunch
Fast Pulse
“Super-fast” injection scheme, on-axis
Septum
Stored beam on-axis
Injected bunch
Super-fast Pulse
Simplified illustration of “Super-fast” on-axis injection scheme
Injected bunch joins the stored bunch
Injected bunch joins the stored bunch
A portion of the stored beam (15 bunches in the illustration) and the injected bunch are deflected with a short kicker pulse (20..30 ns) to fit in the machine aperture. With decaying Betatron oscillation they come back on axis.
A very short kicker pulse (<2 ns) puts an off-momentum injected bunch on-axis without significantly disturbing the adjacent stored bunches. With decaying Synchrotron oscillation the injected bunch joins a stored one.

## Slide 4
Split septum design with and electrical corrector in the middle
Soft magnetic material sandwich-shielding for the stored beam
SLS 2.0 Permanent Magnet-based Thick Septum
  Thick septum 3D model
Parameter | Thick Septum
Gap, mm | 10
Magnet length, m | 2x 0.35
Bending angle, mrad | 120@2.7 GeV
Field integral, T.m | 1.1
Gap field. T | 1.57
Permanent magnets’ type | Sm2Co17
Target zero-field integral, μT.m | 50
Shielding coefficient, - | >20000
Stability, ppt | ±0.1
  Thick Septum Specification
Permanent magnet-based septum will ensure the necessary deflection and stability of the injected beam benefiting from practically maintenance-free operation. Advance magnetic materials like CoFe high magnetic saturation alloys make possible to screen the dipole field in the stored beam region.

## Slide 5
Field strength
The development of strong rare-earth magnets makes possible to create more compact and consumption-free magnetic devices.
Good understanding of magnetic circuits behavior is essential for the design of permanent magnet-based accelerator components.
Remanence limits of the more common strong permanent magnets:
NdFeB – up to 1.5 T
Sm2Co17 – up to 1.2 T
Magnet material has practically free space permeability (is an additional “gap” in the magnetic circuit)
Using “flux concentration” technique the gap field can be made higher than the maximum magnet field (in the expense of massive increase of the necessary magnet volume)
  Magnetic gap
  Magnetic “gap”
S
N
Electrically driven magnetic device
Permanent magnet driven magnetic device

## Slide 6
Temperature sensitivity
NdFeB – 0.9-1.2 ppt/K
Sm2Co17 – 0.3-0.5 ppt/K
Reversable field change
(Is permanent magnet really “permanent”)
  Absolute field vs temperature of different Sm2Co17 alloys [3]
Permanent magnets lose their strength with increasing temperature and gain strength with reducing the temperature (within their operation temperature range)
  Relative field temperature sensitivity of NdFeB and different Sm2Co17 alloys [3]

## Slide 7
Irreversible field change
(Radiation degradation)
  Magnetic field degradation under neutron exposure for different magnet types [4]
Permanent magnets irreversibly degrade under irradiation with high energy photons and particles.
There are different attempts to evaluate their degradation. Nevertheless, a high confidence assessment is difficult due to poorly defined conditions and difficulty to recreate realistic configurations.
  Reduction of magnetic field under neutron exposure for different magnet types [5]

## Slide 8
Radiation damage considerations
Design constrains for dipoles construction – magnets should not be placed in red hatched areas
Careful radiation analysis should be done to define the radiation dosage.
Local shielding can improve (or worsen) the situation.
Place permanent magnets blocks as much as possible away from the beams.

## Slide 9
Beam dump related radiation (horizontal plane)
Neutron fluence at first (upper graph) and second (lower graph) permanent magnet-based septum dipole
  Courtesy of I. Besana
Radiation levels should not cause permanent magnets’ magnetic field degradation.

## Slide 10
0 T
2 T
Shielding with soft magnetic material
  Dipole – shield configuration
Two-stage shielding of Armco iron and Permenorm5000 (FeNi) reduces B down to a few micro Tesla.
The thick septum is ordered
at Arnold Magnetic Technologies
  Field on the shield outer layer
0 T
6 µT
  Shield construction
  Courtesy of G. Martinek (Arnold Magnetic Technologies)
  Field inside the shield

## Slide 11
SLS 2.0 PM-based Thick Septum
  Main field
  B, T
  Z, mm
+5A
-5A
0A
Field Integral
(for given corrector setting):
+5 A: 1.22 T.m (2.7%)
0 A: 1.19 T.m
-5 A: 1.15 T.m (-3.1%)
Leakage field Integral
(for given corrector setting):
+5 A: 94 μT.m
0 A: 84 μT.m
-5 A: 76 μT.m
  Leakage field
  B, T
  Z, mm
+5A
-5A
0A
Earth magnetic field
  Magnetic simulation
  Smallest distance between beams ~35 mm.
  Air gap is important.
Bmax = 2.2 T
Combine magnetic performance

## Slide 12
SLS 2.0 Thin Septum
  Cu
  Cu
Parameter | Thin Septum
Septum thickness, mm | 1.0
Magnet length, m | 0.3
Gap, mm | 6.0
Magnet length, m | 0.3
Bending angle, mrad | 15@2.7 GeV
Field integral, T.m | 0.135
Gap field. T | 0.45@2.7 kA
Pulse length (period), μs | 12.5 (full sine)
Maximum zero-field integral, μT.m | 2.37
Shielding coefficient, - | >50000
Stability, ppt | 1.2
  Thin Septum Specification
Distance between injected and stored beam only 3 mm.
Very thin septum wall - 1 mm
Good magnetic screening
Very thin eddy current septum should ensure inserting the injected beam very close to the stored beam with preferably no disturbance.
  Three sections of SLS 2 thin septum prototype 3D CST® magnetic model
Septum wall
Stored beam
(Line 1)
Injected beam
(Line 2)

## Slide 13
Eddy current septum numerical simulations
Powder cores are chosen for the magnetic circuit to cover the frequency and the filed strength requirements.
3D electromagnetic numerical simulations were used to optimize the screening of the thin septum.
The credibility of the simulation results depends a lot on the correct material model. Choosing the proper material model parameters proved itself difficult since this information is usually not readily available.
  Legend:
  Septum’s 4-layers
  Cu
  Cu
Ip = 3 kA
  Electromagnetic model of the thin septum
  Courtesy of S. Dordevic
Skin depth
  Septum
  “0”-field
  Main field
  Fe-powder core
  Fe-powder core
  Gap 6 mm
  Excitation pulse

## Slide 14
Proper meshing is crucial to get consistent results.
Meshing matters
[T]
[T]
[T]
Tetrahedrons 593’680
Tetrahedrons 190’947
Tetrahedrons 334’662
Influence of mesh on CST results
[uT]
  Courtesy of S. Dordevic
Leakage field results for different mesh density (same other conditions)
Leakage field amplitude vs number of mesh cells

## Slide 15
One mm of cooper does not provide the required screening. No other engineering material (at room temperature) could provide much better conductivity. (Silver is only ~6% more conductive and will not give significant skin depth reduction.)
  Legend
Excitation
Leakage Field in (0/0/0)
Main Field in (0/-10/0)
Main Field along curve 2 @ 22.25us
Leakage Field along curve 1 @ 60us
Copper, thickness 1mm
0.5 mT or 150 µT.m
Conductivity limitation

## Slide 16
Cooper sheet screens the majority of the field. Adding high-µ soft magnetic material we can beat copper in the frequency range where it has available significantly large relative permeability. This compensates its lower conductivity and overall reduces the skin depth.
  Legend
Excitation
µ-metal, thickness 0.15mm
µ-metal, thickness 0.25mm
Copper, thickness 0.3mm
Copper, thickness 0.3mm
Main Field in (0/-10/0)
Main Field along curve 2 @ 22.25us
Leakage Field in (0/0/0)
Leakage Field along curve 1 @ 25.625us
0.7 µT or 0.21 µT.m
Going beyond cooper
Skin depth

## Slide 17
Eddy current barrier is not magnetic field “insulator”!
The field propagates slowly through the septum structure and its maximum can appear much later.
(Electromagnetic wave travels very slowly through the material )
  Legend
µ-metal, thickness 0.15mm
µ-metal, thickness 0.25mm
Copper, thickness 0.3mm
Copper, thickness 0.3mm
Story is a bit more complicated
0 ms 1 ms 2 ms
Leakage Field in (0/0/0)
2.3 µT or 0.69 µT.m
Work in progress

## Slide 18
Conclusions and discussion
Thick septum (permanent magnet based)
Rare-earth permanent magnets dipoles combined with high-saturation soft magnetic screen give a good alternative to pulsed septa.
Nevertheless, the magnetic screening requires larger beam separation.
Thin septum (pulsed)
Combination of copper and µ-metal sheets can provide very good eddy current screening with total septum thickness down to 1.0 mm and respective beam separation of 3.0 mm.
Eddy current screen is not a magnetic “insulator”. Leakage field maximum could appear after ms.
Simulation and measurement of the leakage field is challenging.

## Slide 19
Thank you for your attention

## Slide 20
[1] A. Streun, “SLS-2 Conceptual Design Report”, 2017
[2] A. Streun, “SLS 2.0, The Upgrade of the Swiss Light Source”, IPAC2022, Bangkok, Thailand, 2022
[3] Temperature Compensated Rare Earth Magnets, Arnold Magnetic Technologies
[4] H. Chen et al., “The Effect of Neutron Irradiation on Nd–Fe–B and Sm2Co17-Based High-Temperature Magnets”, IEEE Transactions on Magnetics, Volume: 41, Issue: 10, 2005
[5] B. Shepherd, “Radiation damage to permanent magnet materials: A survey of experimental results”, CERN-ACC-2018-0029 ; CLIC-Note-1079
[]